## Slide 1: Atomic-Level Materials Simulation
Kenan Song
School of Chips
Email: Kenan.Song@xjtlu.edu.cn
Office: C5007
Module Code: MES306TC
Notes: English Title: Uppercase, Calibri size 60, XJTLU Navy
English Subtitle: Uppercase, Calibri size 36, XJTLU Navy

## Slide 2
Bloch’s Theorem, Multi-Sublattice Transformations & 1D Chains
I. Crystal Translational Symmetry & The Bloch Theorem
II. Constructing the Tight-Binding Bloch Sum
III. Monatomic 1D Chain
IV. Crystals with a Basis: The Multi-Sublattice Problem
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 3
Review:
Lattice Translation Vector: , where, are primitive vectors
Periodic Potential: The crystal potential satisfies , which implies the Hamiltonian commutes with the translation operator:
I. Crystal Translational Symmetry & The Bloch Theorem
Translation Operator (TR): Defines the spatial displacement of a wavefunction by a lattice vector R
Physical Consequence: According to quantum mechanics, commuting operators share a simultaneous set of eigenstates. Therefore, the energy stationary states must also be unique eigenstates of the translation operator
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 4
4
I. Crystal Translational Symmetry & The Bloch Theorem
Boundary Condition: Consider a macroscopically large but finite crystal with Ni cells along each primitive direction
Apply the periodic boundary condition
⇒
Solving the Eigenvalue: This enforces , which means must be a root of unity:
where, is an integer
Defining the Wavevector k: For a general lattice vector , the accumulated eigenvalue is:
where, and is the lattice vector of unit cell within the reciprocal space

## Slide 5
The Redundancy Paradox: Let G be a reciprocal lattice vector satisfying
Shift the wavevector k by G, the translation eigenvalue remains completely unchanged
I. Crystal Translational Symmetry & The Bloch Theorem
where, k is the crystal wavevector confined within the First Brillouin Zone ( BZ)
Bloch's Theorem: The eigenstates of a periodic system must satisfy
Physical Meaning: k and k + G describe the exact same physical quantum state with identical translation symmetry
The First Brillouin Zone ( BZ): To eliminate this mathematical redundancy, one restricts all unique k vectors to the unique Wigner-Seitz cell of the reciprocal lattice—the First Brillouin Zone
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 6
The Problem: Raw atomic orbitals do not satisfy Bloch's theorem individually
The Solution (Bloch Sum): Linearly combine atomic orbitals across all lattice sites with a phase factor
II. Constructing the Tight-Binding Bloch Sum
where, N is the total number of unit cells
Under the orthogonal Bloch sum basis, , calculate the k dependent Hamiltonian matrix element
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 7
7
Using lattice translational invariance, let :
The Secular Equation:
II. Constructing the Tight-Binding Bloch Sum
where, is the real-space hopping integral
Standard format of the tight-binding Hamiltonian matrix

## Slide 8
8
System Geometry: A 1D array of identical atoms separated by lattice constant a
Real space lattice vectors
III. Monatomic 1D Chain
Basis: One single s orbital per atom (α = 1)
H(k) will be a 1×1 matrix (a scalar)
TBM Parameters:
On-site energy:
Nearest-neighbor (NN) hopping:
All further hoppings, (2a, 3a, …), are truncated to 0

## Slide 9
Total Hamiltonian matrix is
III. Monatomic 1D Chain
On-site energy:
Nearest-neighbor (NN) hopping:
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 10
Solving the Hamiltonian and obtain the eigenstate and eigenvalue
Boundary Conditions: k is confined within the First Brillouin Zone:
III. Monatomic 1D Chain
Band Structure
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 11
Bandwidth:
Group Velocity:
III. Monatomic 1D Chain
Effective Mass:
Bottom of band (k = 0):
Top of band (k = 0):
(parabolic electron-like)
(hole-like)
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 12
Crystal Structure in reality: Bravais Lattice ⊗ Basis (Atomic Cluster)
The Non-Bravais Reality: Many of the most vital materials in spintronics and valleytronics—such as Graphene (Hexagonal), Silicon (Diamond), and MoS2—are NOT Bravais lattices
They consist of multiple interpenetrating Bravais sublattices
Bravais Lattice: A purely mathematical array of points where every single point has an identical geometric environment (e.g., 1D monatomic chain, Simple Cubic)
IV. Crystals with a Basis: The Multi-Sublattice Problem
Crystal Structure = Bravais Lattice + Basis
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 13
One cannot use a single, global Fourier transform to diagonalize the Hamiltonian. If one forces them into a single Bloch sum, the matrix elements will lose their phase tracking, leading to mathematically incorrect band structures
In a monatomic crystal, every atom is located precisely at Rn. The translation vector connects all atoms and Bloch Sum applies for such case; while, in a crystal with a basis, atoms are located at Rn + τμ. The distance between atom A and atom B inside the same unit cell is τB - τA, which is NOT a lattice translation vector. Under such case, Bloch Sum does not work any longer
The Consequence
IV. Crystals with a Basis: The Multi-Sublattice Problem
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 14
Construct independent Bloch sums for each sublattice separately:
IV. Crystals with a Basis: The Multi-Sublattice Problem
Define the position of an atom as: , where is the unit cell vector, and is the internal coordinate of sublattice μ (e.g. μ = A, B)
Crucial Definition Note: The phase factor inside the sum uses the unit cell position: , NOT the exact atomic position
This is the standard convention for multi-sublattice TBM
Solution:
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 15
Intra- v.s. Inter- Sublattice Matrix Elements
The generalized Hamiltonian matrix H(k) now has a block structure index by sublattices (α, ν)
Diagonal Elements (Hαα): Represent Intra-sublattice hopping (hopping within the same sublattice) and on-site energies
IV. Crystals with a Basis: The Multi-Sublattice Problem
Off-Diagonal Elements (Hαν, α≠ν): Represent Inter-sublattice hopping (hopping from sublattice α to sublattice ν)
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 16
A
Definition: Only consider hopping between atoms that are immediate geometric neighbors. All for , and higher coordination shells are set to exactly zero
IV. Crystals with a Basis: The Multi-Sublattice Problem
B
A
B
A
B
Matrix Form
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 17
IV. Crystals with a Basis: The Multi-Sublattice Problem
-E
-E
det
= 0
Band Gap:
Notes: Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black

## Slide 18
That's all for this session
Thank you for your attention and great participation
Notes: Images should be RGB colour setting
Header: Uppercase, Calibri size 28, XJTLU Navy
Body Text: Sentence case, Calibri size 14, Black